	Test
	Method
	Leading Acrylic Brand

CORIAN
	Quarrystone Series1000 
	Quarrystone Series2000-4000

	Specific Gravity gr./cm3
	ASTM D792
	1.8
	1.79 
	1.732

	Hardness, Barcol
	ASTM D2583
	66
	62-65 
	62-64

	Tensile Strength (psi)
	ASTM D638
	N/A
	7699
	7061

	Tensile Mod. (x10)
	ASTM D638
	1.5
	1.3
	1.1

	Elongation %
	ASTM D638
	.40
	.7 
	.6

	Gloss
	ASTM D638
	5-20
	N/A
	N/A

	Abrasion Resistance: Wt. 

Loss (grams) cycles
	ASTM D4060
	N/A
	.08

500
	.12                    

500

	Wear Thickness (in.) 2000 cycles
	ASTM D4060
	N/A
	.002 
	.002

	Water Absorbtion (Wt.,%/24 hrs.)
	ASTM D570
	+.0400
	+.0254
	+.0356

	Impact IZOD (ft. lb. In.)
	ASTM D256
	.28
	1.00
	.78

	Impact, Falling Ball.... 

1/2 lb. ball
	ANSI Z. 124
	NO EFFECT 3 FEET
	NO EFFECT9 FEET
	NO EFFECT 9FEET

	Thermal Expansion (in./in./F.)
	ASTM D696
	3.02
	2.30 
	2.42

	ARC Resistance (sec)
	ASTM D495
	N/A
	187.5
	184.2

	Oxygen Index
	ASTM D2863
	N/A
	41.0
	35.4

	Heat Resistance
	NEMA LD-3
	PASS
	PASS
	PASS

	Boiling Water Resistance
	NEMA LD-3
	PASS
	PASS
	PASS

	Stain Resistance
	ANSI Z. 124
	N/A
	PASS
	PASS

	Chemical Resistance
	ANSI Z. 124
	N/A
	PASS
	PASS


